##### ﺍلجمهوﺭ ية ﺍلجزﺍئر ية ﺍلديمقرﺍطية ﺍلشعبية وﺯﺍﺭﺓ ﺍلتعليم ﺍلعالي وﺍلبحث ﺍلعلمي

Faculty of Sciences

MASTER’S THESIS

Domain: Matter Science

Field: Physics

Specialty: Materials Physics

Crystallization and Structural Analysis of

Calcium­Based Ceramics in the CaO – Al2O3 – SiO2 System

Defended By: AYA Harche

### On: June 14, 2025

Jury Members:

Mr Youcef Medkour  Setif 1 university ­ MCA ­ President   Mr Mounir Reffas   Setif 1 university ­ MCA ­ Examiner   Mrs Nadjet Aklouche  Setif 1 university ­ MCA ­ Supervisor

Academic Year: 2024/2025

Table of Contents

Table of Contents

Table of Contents	1

General Introduction	3

Chapter I: Ceramic Materials and Properties

  - Introduction	5

  - Overview and classification of ceramics	6

    - Definition of ceramics	6

    - Traditional ceramics	7

    - Technical ceramics	8

      - Types of technical ceramics	8

  - Raw materials for traditional ceramics	9

  - Ceramics compound	10

    - Chemistry of ceramics	10

    - Silicate ceramics and non-silicate ceramics	11

  - Kaolinite minerals	11

    - Kaolinite	12

      - General information	12

      - Kaolinite structure	12

      - Morphology	13

  - Conclusion	13

Bibliography of chapter I	15

Chapter II: Experimental Techniques

  - Introduction	16

  - Ceramic’s synthesis process	16

    - Generalities	16

  - Powder Preparation	16

    - Raw material weighing	16

    - Wet milling	16

    - Calcination	18

    - Second milling	18

    - Powder shaping	18

    - Sintering	18

  - Thermal analyses	19

  - Structural characterization	20

    - X-ray diffraction XRD	20

    - Applications	20

    - Bulk density measurement	21

    - Particle Size	21

    - Infrared spectroscopy study	22

  - Scanning electron microscopy (SEM)	22

Bibliography of chapter II	24

Chapter III: Raw Materials

  - Introduction	25

  - Kaolinite	25

    - Chemical composition	25

    - Mineralogical composition	26

    - Differential Thermal analysis DTA-TGA	27

    - Particle size	29

  - Calcium hydroxide	30

    - X-ray diffraction analysis	30

    - Differential thermal Analysis	31

    - Particle size	32

  - Conclusion	32

Bibliography of chapter III	34

Chapter IV: Results and discussions

  - Introduction	36

  - Addition of Ca(OH)2 and Halloysite	36

  - Particle size distribution	36

  - Ternary diagramme CaO-Al2O3-SiO2	37

  - Thermal Analysis	38

  - X-ray Diffraction	40

    - Crystallite Size (D) and Strain ()	41

  - Bulk density	42

  - Infrared Spectroscopy (FTIR)	43

    - Identified FTIR Bands	43

  - Scanning Electron Microscopy (SEM)	45

  - Conclusion	46

Bibliography Of Chapter IV	47

General Conclusion	48

Abstracts	49

# Abstracts

### Résumé en français

Le présent travail porte sur l’étude d’un système céramique obtenu par combinaison de halloysite et de chaux hydratée [Ca(OH)₂], dans le but de former des phases cristallines au sein du système ternaire CaO-Al₂O₃-SiO₂. L’ajout de 20 % en masse de Ca(OH)₂ permet de modifier la composition de base de l’aluminosilicate et de favoriser la formation de phases d’intérêt telles que l’anorthite (CaAl₂Si₂O₈) et la mullite (Al₆Si₂O₁₃), deux phases très recherchées dans les applications céramiques avancées. Pour comprendre l’évolution des phases et de la microstructure dans ce système, différentes techniques expérimentales ont été utilisées, telles que l’analyse thermique (ATG/ATD), la diffraction des rayons X (DRX), la spectroscopie infrarouge  (FTIR), la microscopie électronique à balayage (MEB) ainsi que l’exploitation du diagramme ternaire CaO-Al₂O₃-SiO₂. La synthèse, le comportement au frittage et les propriétés structurales ont été étudiés entre 1000 °C et 1300 °C.

### ملخص بالعربية

يتناول هذا العمل دراسة نظام ﺧﺰﻓﻲ ﺗﻢ الحصول عليه عن طريق الجمع بين الهالويسيت والجير المطفأ[Ca(OH)₂] ، بهدف ﺗكوين أطوار بلورية داﺧل النظام الثلاثي CaO-Al₂O₂O₃-SiO₂ وﺗسمح إضاﻓة %20 ﻣﻦ ﻛتلة ₂ Ca(OH) بتعديل الترﻛيب اﻷساسي للالوﻣينوسيليكات وتعزز ﺗكوين المراحل ذات اﻷهمية ﻣثل اﻷنورثيت (CaAl₂Si₂O₈) والموليت (Al₆Si₂O₁₃)، وهما ﻣرحلتان ﻣطلوبتان بشدة ﻓﻲ ﺗطبيقات الخزﻓيات الحديثة. ولفهم ﺗطور المراحل والبنية المجهرية ﻓﻲ هذا النظام، ﺗﻢ استخدام ﺗقنيات ﺗجريبية ﻣختلفة، ﻣثل التحليل الحراري(ATG/ATD)، وحيود اﻷشعة السينية(DRX)، والتحليل الطيفي باﻷشعة ﺗحت الحمراء(FTIR) ، والفحص المجهري اﻹلكتروني بالمسح الضوئﻲ(SEM) ، باﻹضاﻓة إلى استغلال المخطط الثلاثي CaO-Al₂O3-SiO2 ﺗمت دراسة الترﻛيب وسلوك التلبيد والخصائص الهيكلية بين1000 درجة ﻣئوية و1300 درجة ﻣئوية.

### Abstract in English

The present work deals with the study of a ceramic system obtained by combining halloysite and hydrated lime [Ca(OH)₂], with the aim of forming crystalline phases within the ternary system CaO-Al₂O₃-SiO₂. The addition of 20% by mass of Ca(OH)₂ modifies the basic composition of the aluminosilicate and promotes the formation of phases of interest such as anorthite (CaAl₂Si₂O₈) and mullite (Al₆Si₂O₁₃), two highly sought-after phases in advanced ceramic applications. To understand phase and microstructure evolution in this system, various experimental techniques were used, such as thermal analysis (ATG/ATD), X-ray diffraction (DRX), infrared spectroscopy (FTIR), scanning electron microscopy (SEM) as well as the exploitation of the CaO-Al₂O₃-SiO₂ ternary diagram. Synthesis, sintering behavior and structural properties were studied between 1000°C and 1300°C .