الجمهورية الجزائرية الديمقراطية الشعبية

وزارة التعليــم العالــي والبحــث العلمــي

جامعـــة سطيـــف 1 فرحـــات عبــــاس

Sétif 1 University- Ferhat ABBAS

كليـــــــــــة الـعـلـــــــــــــــوم

Faculty of Sciences

قســــــــــم الكيمياء

Department of chemistry

Faculty of Sciences

MEMOIRE DE MASTER

DOMAINE:     Sciences de la Matière

FILIERE:          Chimie

SPECIALITE:  Chimie physique

# Thème

Étude de l'efficacité inhibitrice des composés  dérivés du  1,2,4 triazole sur l'acier XC45 en milieu HCl 1 M.

Présenté Par : Badache Islam Dhia Eddine	Encadré Par :  Pr. F. SETIFI

Date de soutenance:18/05/2024

Jury de Soutenance

Président :Dr. A. ADALA

Examinateur :Dr. A. S. MESSALTI

Promotion: 2023/2024

Résumé

L'objectif de ce travail est d'étudier l'inhibition de la corrosion de l'acier XC45 dans le milieu HCl 1M par l'inhibiteur Le 2-Methoxy-4-([1,2,4] triazol-4-yliminomethyl)-phenol et 4-Methoxy-benzylidene-[1,2,4]triazol-4-yl-amine, en utilisant diverses techniques : les méthodes électrochimiques stationnaires (gravimétrieet courbes de polarisation), ainsi que les méthodes électrochimiques non-stationnaires (spectroscopie d'impédance électrochimique). L'influence de la concentration et de la température ont été examinées.

Les résultats ont montré que l'acier XC45 présente un meilleur comportement en milieu HCl 1M avec l'ajout de l'inhibiteur, comme en témoignent les faibles valeurs du potentiel de corrosion (Ecorr) et du courant de corrosion (icorr), ainsi que l'augmentation de la résistance de polarisation (Rp) et de la résistance de transfert de charge (Rtc). L'actions inhibitrices du 2-Methoxy-4-([1,2,4] triazol-4-yliminomethyl)-phenol et 4-Methoxy-benzylidene-[1,2,4]triazol-4-yl-amine sont liées à la formation rapide d'un film protecteur, constituant une barrière au passage du courant de corrosion. Une efficacité maximale de 66.2 %  et 79.6%  a été obtenue à une concentration de 10-3 M pour les deux inhibiteurs respectivement, mais cette efficacité diminue avec l'augmentation de la température. Indiquant que le type d'adsorption est de nature physique et que l'inhibiteurs joux une rôle inhibitrice mixte

.

Les mots clés : Corrosion, Acier XC45, Inhibiteur de corrosion, 1M HCl .

Abstract

The objective of this work is to study the corrosion inhibition of XC45 steel in 1M HCl medium by the inhibitors 2-Methoxy-4-(triazol-4-yliminomethyl)-phenol and 4-Methoxy-benzylidene-triazol-4-yl-amine, using various techniques: stationary electrochemical methods (gravimetry and polarization curves), as well as non-stationary electrochemical methods (electrochemical impedance spectroscopy). The influence of concentration and temperature were examined.

The results showed that XC45 steel exhibits better behavior in 1M HCl medium with the addition of the inhibitor, as evidenced by the low values of corrosion potential (Ecorr) and corrosion current (icorr), as well as the increase in polarization resistance (Rp) and charge transfer resistance (Rtc). The inhibitive actions of 2-Methoxy-4-(triazol-4-yliminomethyl)-phenol and 4-Methoxy-benzylidene-triazol-4-yl-amine are related to the rapid formation of a protective film, constituting a barrier to the passage of the corrosion current. A maximum efficiency of 66.2% and 79.6% was obtained at a concentration of 10-3 M for the two inhibitors respectively, but this efficiency decreases with increasing temperature. Indicating that the type of adsorption is physical in nature and that the inhibitors play a mixed inhibitive role.

Keywords: Corrosion, Steel XC45, Corrosion inhibitor, 1M HCl.

ملخص

الهدف من هذا العمل هو دراسة تثبيط تآكل الصلب XC45 في وسط HCl 1M باستخدام المثبطين 2-ميثوكسي-4-(1,2,4-تريازول-4-يليمينوميثيل)-فينول و 4-ميثوكسي-بنزيليدين-تريازول-4-يل-أمين، باستخدام تقنيات مختلفة: الطرق الكهروكيميائية الساكنة (الوزن الحجمي ومنحنيات الاستقطاب)، وكذلك الطرق الكهروكيميائية غير الساكنة (مطيافية المعاوقة الكهروكيميائية). تم فحص تأثير التركيز والحرارة.

أظهرت النتائج أن الصلب XC45 يظهر سلوكًا أفضل في وسط HCl 1M مع إضافة المثبط، كما يتضح من القيم المنخفضة لجهد التآكل (Ecorr) وتيار التآكل (icorr)، وكذلك الزيادة في مقاومة الاستقطاب (Rp) ومقاومة انتقال الشحنة (Rtc). ترتبط الفعالية التثبيطية لـ 2-ميثوكسي-4-(1,2,4-تريازول-4-يليمينوميثيل)-فينول و 4-ميثوكسي-بنزيليدين-تريازول-4-يل-أمين بتكوين طبقة واقية سريعة، تشكل حاجزًا أمام مرور تيار التآكل. تم الحصول على كفاءة قصوى تبلغ 66.2% و 79.6% عند تركيز 103 مول/لتر للمثبطين على التوالي، ولكن تنخفض هذه الكفاءة مع ارتفاع درجة الحرارة. مما يشير إلى أن نوع الامتزاز هو طبيعة فيزيائية وأن المثبطات تلعب دورًا تثبيطيًا مختلطًا.

الكلمات المفتاحية: التآكل، الفولاذ XC45 ، مانع التآكل، حمض الكلور.

Sommaire

Introduction générale............................................................................. ............................................................................. ............................................................................. ....................................../... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ......................................................................01

Chapitre I : Rappel Bibliographie

I.1. Notion générale sur la corrosion ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ....................................................................04

I.1.1. Définition de la corrosion............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .............................................................................04

I.1.2. Processus de corrosion ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ......................................... 04

I.1.3. Types de corrosion .............................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .................................................. ............................... 05

I.1.3.a. Corrosion chimique (sèche) ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::::::::05

I.1.3.b. Corrosion biologique (bactérienne) ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................... ::::::06

I.1.3.c. Corrosion par érosion ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::::::::::::::::::::::::06

I.1.3.d. Corrosion électrochimique (humide) ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::07

I.1.4. Formes de corrosion ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .................................... ::07

I.1.4.a. Corrosion uniforme ou généralisée............................................................................. ................................................................... ::....................................................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ........................................................................ 07

I.1.4.b. Corrosion localisée ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::::::::08

I.1.4.c. Corrosion caverneuse ou parcrevasse............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::::09

I.1.4.d. Corrosion intergranulaire............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ........................................ ::::::::::..................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ................................................................... :10

I.1.4.e. Corrosion sous contrainte ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .................................................... :::::::::::10

I.1.4.f. Corrosion sélective ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::::::::::::11

I.1.4.g. Fragilisation par hydrogène ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ....................... ...................................................... ............................................................................. ............................................................................. ............................................................................. :::::::::::11

I.1.5. Principaux facteurs responsables de la corrosion............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ...................................... ::12

I.1.6. Moyens de protection contre lacorrosion ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .. ........................................................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ::::::::13

I.1.7. La protection contre la corrosion............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ::::::::::15

I.2. Généralités sur les inhibiteurs de corrosion ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ::::::::::15

I.2.1. Définition............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .................................................... ::::::16

I.2.2. Propriétés............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ........................................................... ::16

I.2.3. Domaines d’utilisation............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ...................................................... 17

I.2.4. Classification des inhibiteurs ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :17

a. Selon la nature............................................................................. ............................................................................. ............................................................................. ........................////////////............. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ::::::............................................................................. ............................................................................. ............................................................................. ............................................................................. ::::::::::18

a.1. Inhibiteurs organique ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .......................... ::::::::................................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................ 18

a.2. Les inhibiteurs minéraux ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ................................................... ::::::::::.......................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ..................................... :18

b. Selon nature électrochimique du processus............................................................................. ............................................................................. ............................................................................. .///////................................................... ................................................................................................................................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ................................................... :19

b. 1. Inhibiteurs anodiques............................................................................. ............................................................................. ............................................................................. ..... ............................................................................. ............................................................................. ............................................................................. :::::::........................................................................ ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. :::::::::::::19

b. 2. Inhibiteurs cathodiques............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. 19

b. 3. Les inhibiteurs mixtes............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ::::::::::19

c. Selon le mécanisme en fonction de mode d’action............................................................................. ....................... ............................................................................. ........................... :.................................................. ............................................................................. ............................................................................. ................................................................................................................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. 20

c. 1. Par adsorption............................................................................. ............................................................................. ............................................................................. ..................................//////////........................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .....................................//////////////////////........................................ ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .............................................................................20

I.2.5. Effet de température............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ......................................//////////////////....................................... ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. 21

I.2.6.Influence de la concentration sur l’effet inhibiteur............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. //////////22

- Langmuir............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ................................................////............................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .........................................................22

- Temkin ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ////22

I.2.7.Inhibiteurs de corrosion en milieu acide............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .........................................................23

I.2.8. Analyse bibliographique ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ////23

I.2.9. Propriétés physico-chimiques des triazole ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ...........................................................................24

I.2.10. Motivation dans le choix de ligand dérivé de 1,2,4Triazole comme inhibiteur de corrosion .................................................///////////24

Référence Bibliographies ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. .........................26

Chapitre II : Techniques et méthode utilisées.

Introduction ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ..................................................//28

II.1. Étude de l’inhibition de l’acier XC45............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ............................................................................. ..........................................////28

II.1.1. Matériau .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..................................../28

II.1.2. Matériels utilisés.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ................................./28

II.2. Réactifs et solvants .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................//////////////29

II.2.1. Vanilline .............................................. .............................................. .............................................. ............................... .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................29

II.2.2. Triazol .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .....................///29

II.2.3. Montage de synthèse .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ....................................../30

II.3.3. Synthèse des2-Methoxy-4-([1,2,4]triazol-4-yliminomethyl)-phenol et 4-Methoxy-benzylidene-[1,2,4]triazol-4-yl-amine.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................////31

II.4. Techniques expérimentales spectroscopiques.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ...........///////................................... .............................................. ............................................................................................ .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................32

II.4.1. La chromatographie sur couche mince (CCM.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................................../////////32

II.4.2.  Spectroscopie infrarouge (IR)............................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................33

II.4.3. Spectrophotométrie Ultra Violette-Visible (UV-Visible) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ........................33

II.5. Milieu d’étude .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..../////34

II.6. Condition d’étude électrochimique .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................................../34

- Appareillage .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................////////////////////////35

- Montage électrochimique .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................////////////////35

II.7. Méthodes d’évaluation de corrosions .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................//////36

II.7.1. Méthode gravimétrique .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ......................................//36

II.8. Méthodes électrochimiques .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................37

III.8.1. Méthodes stationnaires .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ................................37

II.8.1.1. Suivi du potentiel en circuit ouvert (OCP) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..........................37

II.8.1.2. Courbes de polarisation .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................................../38

III.8.1.3. Spectroscopie d’impédance électrochimique (SIE) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ...................................//39

a-Représentations graphiques .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................40

b-Circuits équivalents .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................//////////////////////////////41

C-Utilisation de schémas électriques équivalents .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................////42

Références Bibliographies.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................../43

Chapitre III : Résultats et discussion

III.1. Introduction .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ......................................./45

III.2. Propriétés des ligands synthétisés .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................//////////45

III.3. Caractérisations des Inhibiteurs .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................//46

III.3.1. Caractérisations des ligands Trz-O-CH3 et Trz-OH O-CH3.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ........................./46

III.3.1.1. La base de Schiff (Trz-OH-O-CH3) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ........................................./46

A. La spectroscopie Infrarouge (IR) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................................../47

B. Spectrophotométrie UV-vis .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................///////47

III.3.1.2. La base de Schiff (Trz-O-CH3) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ................................/48

A. La spectroscopie Infrarouge (IR) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................................../////////// .............................................. .............................................. .............................................. .............................................. .............................................. ................................./48

B. Spectrophotométrie UV-vis .............................................. ........................ .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................///////...................... .............................................. ..............................................49

III.4. Mesures de perte de poids .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................///////////50

III.5. Mesure chronopotentiométriques .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ................./51

III.5.1. Courbes de polarisations .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ..............................................//51

III.5.2. Spectroscopie d’impédance électrochimique (SIE) .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ........................./54

III.5.3. Effet de la température en milieu HCl 1 M .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ....................................57

III.6.1. Etude théorique .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................60

III.6.2. Calcule de la chimie quantique .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................................../////////////////////62

Références Bibliographies.............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ...............................64

Conclusion générale .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ......///////////////////////////////////////////////////////////////////........................................ .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. .............................................. ............................//////////66