DEMOCRATIC AND PEOPLE’S REPUBLIC OF ALGERIA

Ministry of Higher Education and Scientific Research

University Ferhat Abbas Sétif-1

Faculty of Sciences

Department of Chemistry

DEMOCRATIC AND PEOPLE’S REPUBLIC OF ALGERIA

Ministry of Higher Education and Scientific Research

University Ferhat Abbas Sétif-1

Faculty of Sciences

Department of Chemistry

MASTER’S THESIS

Field: Science of Matter

Specialty: Chemistry-Physics

Study of the Electrocatalytic Properties of Electrodes for Water Electrolysis

Study of the Electrocatalytic Properties of Electrodes for Water Electrolysis

Thesis Title:

Presented by: GHIAT Khouloud	Supervised by: H. BELHADJ

BELILITA Lamise

Thesis defended publicly on 21/06/2025 before the examination committee composed of:

| Committee in charge: |  |  |
| --- | --- | --- |
| President: A. Azizi |
| Examiner: C. Dehchar |
| Supervisor: H. Belhadj |
| Co-supervisor: Y. Messaoudi |

2024/2025

Abstract

In this study, pristine ZnS, ZnFe₂O₄, and their composite ZnS/ZnFe₂O₄ heterostructure were successfully synthesized via a simple electrodeposition method and comprehensively characterized using structural, optical, and electrochemical techniques. X-ray diffraction (XRD) confirmed the crystalline nature and successful formation of as-prepared electrode. UV–Vis spectroscopy and Tauc analysis revealed a shift in the absorption edge of the heterojunction, resulting in a novel band gap of 2.80 eV, enabling visible-light excitation. Mott–Schottky analysis demonstrated the formation of a p–n heterojunction with enhanced charge carrier concentration and a favorable flat-band potential shift, promoting efficient interfacial charge separation. Electrochemical investigation showed superior hydrogen evolution reaction (HER) activity for the ZnS/ZnFe₂O₄ electrode in alkaline media, delivering a low overpotential of 261 mV at −10 mA·cm⁻² and a Tafel slope of 122 mV·dec⁻¹, indicating Volmer-step-dominated kinetics. Electrochemical impedance spectroscopy (EIS) revealed the lowest charge-transfer resistance (2.13 Ω) and the highest electrochemically active surface area (ECSA = 30.25 cm²), suggesting rapid electron transport and abundant active sites. The composite electrode also demonstrated excellent durability, maintaining stable performance after 1500 LSV cycles and 3 hours of continuous operation at −100 mA·cm⁻². Notably, under visible-light irradiation, HER activity was further enhanced due to improved electrical conductivity and efficient charge separation at the ZnS/ZnFe₂O₄ interface. The formation of the p–n heterojunction effectively reduces charge recombination and creates new active sites, significantly enhancing hydrogen production. These findings highlight the potential of heterojunction engineering and establish ZnS/ZnFe₂O₄ as a cost-effective and durable photo and electrocatalyst for sustainable hydrogen generation in alkaline media.

Keywords: Hydrogen Evolution Reaction (HER), ZnS, ZnFe₂O₄, Heterojunction, Electrocatalysis.

الملخص

في هذه الدراسة، تم بنجاح تحضير كل من ZnS النقي، وZnFe₂O₄، بالإضافة إلى المركب غير المتجانس ZnS/ZnFe₂O₄ باستخدام طريقة الترسيب الكهربائي البسيطة. وقد تم توصيف هذه المواد بشكل شامل باستخدام تقنيات بنيوية، وبصرية، وكهروكيميائية. أكد تحليل حيود الأشعة السينية (XRD) على الطبيعة البلورية والتكوين الناجح للقطب الكهربائي المحضَّر. كما كشفت مطيافية الأشعة فوق البنفسجية–المرئية (UV–Vis) إلى جانب تحليل Tauc عن حدوث انتقال في حافة الامتصاص ضمن الوصلة غير المتجانسة، مما أدى إلى ظهور فجوة طاقة جديدة (Band Gap) تساوي 2.80 إلكترون فولت (eV)، وهو ما يسمح بتحفيزها تحت إشعاع الضوء المرئي.أظهر تحليل Mott–Schottky تكوّن وصلة غير متجانسة من النوع p–n، مصحوبة بزيادة في تركيز ناقلات الشحنة (Charge Carriers) وتحول إيجابي في جهد النطاق المسطح (Flat-Band Potential)، مما يعزز بشكل فعال فصل الشحنات على السطح البيني.أظهرت الدراسة الكهروكيميائية أداءً فائقًا لقطب ZnS/ZnFe₂O₄ في تفاعل إنتاج الهيدروجين (HER) في وسط قلوي، حيث سُجل جهد زائد منخفض (Overpotential) قدره 261 ميلي فولت (mV) عند −10 ميلي أمبير لكل سنتيمتر مربع (−10 mA·cm⁻²)، وميل Tafel بلغ 122 mV·dec⁻¹، مما يدل على أن آلية التفاعل تهيمن عليها خطوة فولمر (Volmer step).كذلك، أظهرت مطيافية الإعاقة الكهربائية (EIS) أدنى مقاومة لنقل الشحنة بلغت 2.13 أوم (Ω)، وأعلى مساحة سطحية نشطة كهروكيميائيًا (ECSA) وصلت إلى 30.25 سم² (cm²)، مما يشير إلى وجود نقل إلكتروني سريع وتوفر كبير في المواقع النشطة.كما أثبت القطب المركب مقاومة عالية واستقرارًا ممتازًا، حيث حافظ على أدائه بعد 1500 دورة من اختبار LSV و3 ساعات من التشغيل المتواصل عند −100 mA·cm⁻².ومن الجدير بالذكر أن نشاط تفاعل HER قد تحسَّن بشكل إضافي تحت إشعاع الضوء المرئي، نتيجة لتحسُّن التوصيلية الكهربائية وكفاءة فصل الشحنات عند واجهة ZnS/ZnFe₂O₄. إن تكوين الوصلة غير المتجانسة p–n يساهم بفعالية في تقليل إعادة اتحاد الشحنات وخلق مواقع نشطة جديدة، مما يؤدي إلى تعزيز كبير في إنتاج الهيدروجين. تُبرز هذه النتائج الإمكانات الواعدة لهندسة الوصلات غير المتجانسة (Heterojunction Engineering)، وتُثبت أن ZnS/ZnFe₂O₄ يمثل محفزًا ضوئيًا وكهروكيميائيًا منخفض التكلفة، فعالًا ومستقرًا لإنتاج الهيدروجين المستدام في الوسائط القلوية.

الكلمات المفتاحية:
تفاعل إنتاج الهيدروجين (HER)، ZnS، ZnFe₂O₄، وصلة غير متجانسة، التحفيز الكهروكيميائي.

CONTENTS

List of abbreviation

GENERAL INTRODUCTION1

Reference bibliography 2

Chapter I: Review Bibliography

I.1. General concepts of semiconductors4

I.1.1. Transparent Conductive Oxides (TCOs) 5

I.1.2. Types of semiconductors6

I.1.2.1. Intrinsic semiconductors6

I.1.2.2. Extrinsic semiconductors6

A. N-type Semiconductor6

B. P-type Semiconductor6

I.2. n-p Junctions6

I.2.1. Different types of junctions6

I.2.1.1. Homojunction6

I.2.1.2. Heterojunction7

A. Type-I (Straddling Gap) 7

B. Type-II (Staggered Gap) 7

C. Type-III (Broken Gap) 8

D. Z-Scheme Heterojunction8

I.3.  Approaches to Synthesis8

I.3.1 Top-down Approach8

I.3.2. Bottom-up Approach9

I.4. Properties of semiconductors10

I.4.1. Electricals properties10

I.4.1.1 Conductivity10

I.4.1.2. Resistivity10

I.4.1.3. Bandgap10

I.4.2. Optical properties11

I.5. Applications11

I.5.1. Electrocatalysis for the Hydrogen Evolution Reaction (HER) 12

I.5.2. Photoelectrochemical Cells (PECs) 12

References Bibliography13

Chapiter II: Experimental Section

Ⅱ.1. Properties of the Semiconductor Materials16

Ⅱ.1.1. Zinc Sulfide (ZnS) 16

Ⅱ.1.2. Zinc Ferrite (ZnFe₂O₄)17

II.2. Bath and conditions for developing deposits18

II.3. Experimental Setup for Electrodeposition (ED) 18

II.4. Materials And Reagents19

II.5. Substrate Preparation19

II.6.  Electrodeposition 20

II.6.1. Electrodeposition of ZnS20

II.6.2. Electrodeposition of ZnFe₂O₄20

II.6.3. Fabrication of ZnS/ZnFe₂O₄ Heterojunction Electrodes21

II.7. Mechanism of Electrodeposition21

II.7. 1.Electrodeposition Mechanism of ZnS21

II.7.2. Electrodeposition Mechanism of ZnFe₂O₄21

Reference23

Chapter III: Results and Discussions

III.1. Structural analysis by X-ray diffraction (XRD) 25

III.2. Ultraviolet–Visible Spectroscopy (UV/Vis) 27

III.3. Electrochemical study28

III.3.1. Electrocatalytic HER Performance28

III.3.2. Electrochemical impedance spectroscopy (EIS) measurements31

III.3.3. Stability33

III.4. Mott–Schottky Measurements (M–S) 34

III.5. Photoelectrochemical (PEC) measurements37

III.6. Possible mechanism 39

Reference40

Conclusion42