PEOPLE'S DEMOCRATIC REPUBLIC OF ALGERIA

MINISTRY OF HIGHER EDUCATION AND SCIENTIFIC RESEARCH

UNIVERSITY OF SETIF 1

FACULTY OF SCIENCES

DEPARTMENT OF CHEMISTRY

MASTER DISSERTATION

Submitted in partial fulfillment of the requirements for the Master’s degree in CHEMISTRY

OPTION: Analytical Chemistry

Theme

Analysis of the Properties of Composite Materials by Atomic Force Microscopy

Presented by: Kara Khalissa

Ferdi Dina

Graduation date: 28/06/2025

Jury Members:

President: Dr. A.MADANI, MCB, UNIVERSITY OF SETIF 1

Supervisor: Dr. Y.MESSAOUDI, MCA, UNIVERSITY OF SETIF 1

Co_Supervisor: I. BOUHMILA, LABORATORY MANGER, IRIS TYRES

Examiner: Dr. Y. NOUAR, MCA, UNIVERSITY OF SETIF 1

Academic year: 2024/2025

Abstract

In recent years, the automotive industry, particularly tire manufacturing, has experienced significant development and transformation from a simple rubber strip to a complex system composed of dozens of different materials. This complexity aims to significantly enhance tire performance, with a focus on increasing longevity, durability, and adaptability to various operational conditions. These improvements require a detailed study of the materials used and their manufacturing processes.

In this study investigate the effect of carbon black with different grades on the rheological, mechanical and physical properties of rubber blend SBR/NR.

Carbon black is widely used as a reinforcing filler in rubber composites, enhancing their properties. The grades added and chosen for the various formulations of rubber compounds are N234, N375, N660.

The study evaluates how these three specific grades influence key properties such as tensile strength, elongation at break, hardness, abrasion resistance.

Résumé

Ces dernières années, l'industrie automobile, en particulier la fabrication de pneus, a connu un développement et une transformation significatifs, passant d'une simple bande de caoutchouc à un système complexe composé de dizaines de matériaux différents. Cette complexité vise à améliorer considérablement les performances des pneus, en mettant l'accent Abstract sur l'augmentation de la longévité, de la durabilité et de l'adaptabilité à diverses conditions de fonctionnement. Ces améliorations nécessitent une étude détaillée des matériaux utilisés et de leurs processus de fabrication.

Cette étude examine l'effet du noir de carbone de différents grades sur les propriétés rhéologiques, mécaniques et physiques du mélange de caoutchouc SBR/NR.

Le noir de carbone est largement utilisé comme charge de renforcement dans les composites en caoutchouc, améliorant ainsi leurs propriétés. Les grades ajoutées et choisies pour les différentes formulations de mélange de caoutchouc sont N234, N375, N660.

L'étude évalue comment ces trois grades spécifiques influencent les propriétés clés telles que la résistance à la traction, l'allongement à la rupture, la dureté et la résistance à l'abrasion.

الملخص

شهدت صناعة السيارات في السنوات الأخيرة، وخاصة في مجال تصنيع الإطارات المطاطية، تطورًا وتحولًا كبيرين، حيث انتقلت من شريط بسيط من المطاط إلى نظام معقد يتكون من عشرات المواد المختلفة. تهدف هذه التعقيدات إلى تحسين أداء الإطارات المطاطية بشكل كبير، مع التركيز على زيادة العمر الافتراضي، والمتانة، والقدرة على التكيف مع ظروف التشغيل المختلفة. وتتطلب هذه التحسينات دراسة مفصلة للمواد المستخدمة وعمليات التصنيع الخاصة بها

في هذا العمل ، تم دراسة تأثير الكربون الأسود بدرجاته المختلفة على الخصائص الريولوجية والميكانيكية والفيزيائية لمزيج المطاط   SBR/NR. 
يُستخدم الكربون الأسود على نطاق واسع كمادة مالئة معززة في مركبات المطاط، حيث يُحسن من خصائص وإضافتها إلى تركيبات مختلفة من مركبات المطاط تم اختيار الدرجات N234, N375, N660
 
تُقيِّم الدراسة كيف تؤثر هذه الدرجات الثلاثة المحددة على الخصائص الرئيسية مثل قوة الشد، الاستطالة عند الانقطاع، الصلابة، ومقاومة التآكل

Table of Contents

List of abbreviations..........................................................................................................................

List of figures.....................................................................................................................................

List of tables.......................................................................................................................................

General Introduction........................................................................................................................1

References........................................................................................................................................4

Chapter I: Polymers

I.1.Polymers.....................................................................................................................................5

I.1.1. Definition................................................................................................................................5

I.1.2. Applications............................................................................................................................5

I.1.3. Polymer classification.............................................................................................................6

I.1.3.1. Thermosetting Polymers......................................................................................................6

I.1.3.2. Thermoplastic Polymers......................................................................................................7

I.1.3.3. Elastomers (Cross-linked Polymers) ..................................................................................8

I.2. Rubber.......................................................................................................................................9

I.2.1. Definition................................................................................................................................9

I.2.2. Types......................................................................................................................................9

I.2.2.1. Natural rubber (NR) ............................................................................................................9

I.2.2.2. Synthetic rubber.................................................................................................................11

I.2.4. Rubber Vulcanization...........................................................................................................12

I.2.4.1. Vulcanization based on sulfur...........................................................................................12

I.3. Pneumatic .............................................................................................................................. 13

I.3.1. Introduction......................................................................................................................... 13

I.3.2. History................................................................................................................................. 13

I.3.3.The main layers of a tire........................................................................................................14

I.3.4. Explanation of Tire Markings.............................................................................................. 16

I.3.5. Rubber additives...................................................................................................................17

I.3.5.1.Fillers..................................................................................................................................17

I.3.5.2. Accelerators.......................................................................................................................20

I.3.5.3. Activators...........................................................................................................................20

I.3.5.4. Antidegradents...................................................................................................................20

I.3.6. Impact on the environment and health.................................................................................21

I.3.6.1. Environmental concerns....................................................................................................21

I.3.6.2. Health concerns.................................................................................................................21

References......................................................................................................................................23

Chapter II: Materials and Methods

II.1. Compound Preparation (Mixing Process) .............................................................................26

II.1.1.Cleaning batch......................................................................................................................28

II.1.2.Master batch.........................................................................................................................28

II.1.3.Final batch............................................................................................................................30

II.1.4.Vulcanization.......................................................................................................................31

II.1.5.Testing..................................................................................................................................32

II.2.Quality control tests................................................................................................................32

II.2.1.Mooney viscosity.................................................................................................................32

II.2.2.Rheometer............................................................................................................................34

II.2.3.Tensile..................................................................................................................................36

II.2.4.Dispersion.............................................................................................................................38

II.3.The Invention of AFM............................................................................................................40

II.4.Principle of AFM....................................................................................................................41

II.5.The Force-Distance Curve......................................................................................................42

II.6.AFM Measurement Modes......................................................................................................43

II.6.1.Short-Distance Force Measurement.....................................................................................43

II.6.1.a) Contact Mode...................................................................................................................43

II.6.2.Long-Distance Force Measurement.....................................................................................44

II.6.2.a) Tapping Mode (AC Mode) ..............................................................................................45

II.6.2.b) AMFM.............................................................................................................................45

References......................................................................................................................................47

Chapter III: Results and Discussion

III.1 Mechanical characterizations.................................................................................................48

III.1.1 Mooney Viscosity First and Final Stage.............................................................................48

III.1.2. Rheometric Properties........................................................................................................50

III.1.3.Tensile Properties................................................................................................................53

III.1.4.Hardness Shore A...............................................................................................................57

III.1.5.Dispersion Analysis............................................................................................................59

III.2 Microscopy analysis by AFM................................................................................................63

III.2.1 Detection of CB in Rubber surface by AFM......................................................................64

III.2.2. CB dispersion on Rubber surface......................................................................................67

References......................................................................................................................................71

General conclusion.........................................................................................................................72